AVALIAÇÃO IN VITRO DA CITOXICIDADE DA MEMBRANA DE ALUMINA(Al203).

OBJETIVO: 	O objetivo deste trabalho é fazer uma avaliação in vitro da citotoxicidade da membrana de alumina (Al2O3), utilizando células bastante sensíveis do córtex cerebral de ratos.

Metodologia:	Mínimo 30 casos ou sítios.

1 - utilizar cultura de células do córtex cerebral(neurônios e células da glia) de ratos, preparadas de fetos de 15-16 dias de gestação (Webster Suiço ou outros).

2 - manter as membranas flutuando no meio de cultura, sem tocar nas células para não haver injúria física.

3 - fazer a avaliação de acordo com a sugestão do laboratório ou por contagem de células alteradas ou mortas  por medição de lactato dehidrogenase liberado pelas células lesadas ou mortas, após 24 horas de exposição à membrana.

4 – Estabelecer a metodologia correta segundo o laboratório. Isto é apenas uma sugestão.

# Grupo teste

Grupo Controle

BIBLIOGRAFIA:

Araújo NS, Jaeger RG, Todescan FF, et al. Cell culture test for assessing attachment and proliferation on titanium dental implants with modified surfaces. RPG Rev Pós Grad 2001; 8(2):103-109.

Bowers KT, Keller JC, Randolph BA, et al. Optimization of surface micromorphology for enhanced osteoblast responses in vitro. Int J Oral Maxillofac Implants 1992;7(3):302-310.

Cooper LF, Masuda T, Whitson SW, et al. Formation of mineralizing osteoblast cultures on machined, titanium oxide grit-blasted, and plasma-sprayed titanium surfaces. Int J Oral Maxillofac Implants 1999; 14(1): 37-7.

Cooper LF. A role for surface topography in creating and maintaining bone at titanium endosseous implants. J Prosthet Dent  2000; 84: 522-34.

Cruz M. Regeneração Guiada Tecidual. São Paulo: Santos Editora; 2006.

Garvey BT, Bizios R. A transmission electron microscopy examination of the interface between osteoblasts and metal biomaterials. J Biomed Mater Res 1995;29(8):987-992.

Kasemo B, Lausmaa J. Metal selection and surface characteristics. In:  Branemark P-I, Zarb GA, Albrektsson T. Tissue-integrated prostheses: osseointegration in clinical dentistry. Chicago: Quintessence Publishing Co., Inc., 1985. Chap. 4, p. 99-116.

Malik MA, Puleo DA, Bizios R, et al. Osteoblasts on hydroxyapatite, alumina and bone surfaces in vitro: morphology during the first 2h of attachment. Biomaterials 1992;13(2):123-128.

Prado da Silva MH, Lima JHC, Soares GDA, et al. Avaliação morfológica de osteoblastos humanos cultivados sobre titânio puro e titânio recoberto com hidroxiapatita. Rev Bras Implant 1999; 10-12.